7 Tesla SQUID Magnetometer

(NSF DMR-0113714)

# The Result of the Month

(January 2003)

## Magnetic properties of manganin

E. Cizmar1, J.-H. Park1, M. W. Meisel1, M. Orendáč2

1Department of Physics, University of Florida

2 Institute of Physics, P.J. Šafárik University, Košice, Slovakia

| Fig. 1. Magnetic susceptibility of the field-cooled (FC) and zero field-cooled (ZFC) sample measured in temperature range from 2 to 300 K with H = 1 kG. | Fig. 2. Field dependence of magnetization of the polycrystalline sample at 5 K. |
| --- | --- |

The manganin alloy (82% Cu, 12% Mn, 4% Ni) is often used for wiring in cryogenic apparatus because of small change of the electric resistance in the low temperature region.  Due to the high concentration of magnetic ions, the contribution of manganin itself might be important in magnetic measurements or in experiments involving applied magnetic fields.  Previous studies of diluted CuMn alloys showed spin-glass behavior in these systems [1-3].  In addition, the manganin shows spin-glass behavior with freezing temperature at about 60 K.  The magnetization from 0 to 70 kG shows a S-shape type of curve, typical for spin-glass materials.

Supported by the NSF through INT-0089140 and DGE-0209410

[1] G.E. Brodale et al., JMMM 31-34 (1983), 1331.

[2] P.J. Ford et. al, Phys. Rev. B 14 (1976) 2057.

[3] C.A.M. Mulder et al., Phys. Rev. B 23 (1981) 1384.

Questions or Suggestions e-mail me cizmar@phys.ufl.edu