7 Tesla SQUID Magnetometer

(NSF DMR-0113714)

# The Result of the Month

(September 2002)

## Magnetic Characterization of a Ni-Dimer Material

J.-H. Park*, E. Cizmar*, M. W. Meisel*, C. Liu**, D. R. Talham**

* Department of Physics, University of Florida

** Department of Chemistry, University of Florida

| Fig. 1 χ vs T measured with applied field of 1 kG. The sturucture of NiDi is shown in the inset. | Fig. 2 χT vs T measured with applied field of 1 kG. The inset shows magnetization at T = 2 K measured as a function of applied field. |
| --- | --- |

The result of this month is about “NiDi”, a Ni dimer compound Ni2(dipic)2(C4H4N2) ( (H2O)4, where dipic is dipiclinic acid, C5H3N(CO2)2 and M.W. = 599.74 g/mol, studied in polycrystalline form and synthesized by Chen Liu in Dr. Talham’s group.  The NiDi is possibly a magnetic spin ladder material with weak interactions between Ni2+ (S = 1) centers along the rung and leg directions of ladder.  At first look, a decreasing tail of  χT at low temperature and a constant value of χT in the high temperature range (Fig. 2) suggest that there are antiferromagnetic interactions with a g value ~ 2.05.  The Weiss temperature extracted from a 1/χ vs. T plot (not shown here) is about 1.1 K.  The fact that our NiDi sample is polycrystalline form and the possible axially distorted environment of Ni2+ d8 configuration encourage further study on this material.  This work is partially supported by the ACS-PRF-36163-AC5 and the NSF DGE-0209410.

Questions or Suggestions email me  juhyun@phys.ufl.edu