Homework Solutions 2, PHY4905

Due Wednesday (due to holiday), January 22, 2014

Kittel, Chap. 2, problems 1 and 2

2.) In problem 1, you have found the interplanar (d) spacing for simple cubic.  Polonium, chemical symbol Po, is simple cubic and has a lattice parameter of 3.359 Ǻ (this is the distance between Po-Po nearest neighbors, i. e. this is the lattice parameter for the primitive cell, not some larger conventional cell).  Using the Bragg law for first order reflections (n=1), (=2dsin(, and copper K( radiation with (=1.54 Ǻ

a.) list the first (lowest angle) six reflection d-spacings and the associated Miller indices, (hkl),

dhkl for (hkl)=100, 110, 111, 200, 210, 211   d = a/(h2 + k2 + l2)1/2 = 3.359 Ǻ, 2.375 Ǻ, 1.939 Ǻ, 1.6795 Ǻ, 1.502 Ǻ, and 1.371 Ǻ respectively

b.) list the corresponding ( angles for these first six reflections.

(=sin-1 ((/2d) = sin-1 (0.77/3.359 Ǻ, 2.375 Ǻ, 1.939 Ǻ, 1.6795 Ǻ, 1.502 Ǻ, and 1.371 Ǻ respectively) = 13.25o, 18.92o, 23.40o, 27.29o, 30.84o, 34.17o respectively

4.) Kittel, Chap. 2, prob. 5.